## Slide 1: Materials Development Program
at CSIR-NML

## Slide 2
Magnetic
Materials
Thin Films &
Coating
Biomaterials
Metallic
Glasses
Inhibitors
Structural
Materials

## Slide 3
Fe6.5Si Steel
Ferromagnetic Shape memory Alloy (NiMnGa)
Magnetostrictive
Amorphous Alloys:
FeSiB, CoSiB
Silicon Steels :Fe-6.5Si
Nanostructured ultrasoft Magnetic alloys : FeNbCuSiB
High induction & High Curie temp.Alloys : CoFeSiB
Melt Spinning technology for the production of wide (25mm) ribbons (About 1kg batch)
Technology transferred to M/s Vacuum Techniques, Bangalore, India
Brazing alloys for space application
Brazing foils :
Cu-Ni-Mn , Ti-Zr-Cu-Ni
FeSiB alloy
New CSIR for New India
Magnetic Alloy for Sensors
& Transformer Core

## Slide 4
World Market for Applications of Mag.
Ferrite 34 1 96 %
NdFeB 280 24 1 %
SmCo 150 32 0.5 %
AlNiCo 40 3 2.5 %
Cost
ratio
BHmax
kj/m3
Use
Properties of Some Magnets
Ferrite is a low cost magnet,
but magnetic strength is low
Properties need to improve
for better performance
Hc enhanced by La, & Co doping
5400 Oe to 7800 Oe
Ms, Mr and Hc data of doped SrFe12O19
Magnets fabricated and evaluated
New CSIR for New India
Improvement of Magnetic Strength
of Ferrite Permanent Magnet

## Slide 5
Magnetic Field Induced Strain (MFIS) in annealed FSMA ribbons
Ni55Mn22Ga22Al1
Ni55Mn22Ga23
As-Spun Ni55Mn22Ga23
Mart. Start : MS= 142oC
As-Spun Ni55Mn22Ga22Al1
Mart. Start : MS = 231oC
Martensite Twins
Martensite Plates
New CSIR for New India
Ferromagnetic Shape Memory
Alloys (FSMAs) by Rapid Solidification

## Slide 6
Research Area (PVD, CVD, e-beam, Laser cladding, HVOF, Thermal Spray, Plasma Spray)
Hard & tough coatings for wear resistance applications
High temperature and oxidation resistant coatings
Coatings for corrosion resistance application
Recent Projects
Nanocomposite multicomponent coatings of TiSiBC system for wear resistance and less coefficient of friction applications (Ashok Leyland)
Multilayered hard and tough coatings of SiCN system
Cadmium replacement coatings for landing gears in aeroplane (Boeing International)
Anti corrosion, foul fuel sustainable coatings (Tata Steel)
Anticorrosion and anti bacterial coatings (Tata Steel)
New CSIR for New India
Coatings

## Slide 7
New CSIR for New India
Coatings for various applications
Piston ring of truck engine Ashok leyland
Al2O3-Fe coated pipe
Al2O3-TiB2 coated pipe
Laser cladded hydroturbine guided vanes

## Slide 8
Alloys BMG’s
Size of BMGs produced
Rods: L ~70mm,  up to 3mm
Plates: L ~70mm, B ~8mm, T ~up to 1.5mm
Composition of BMGs produced
Cu-Zr-Ti alloys with minor addition
of Nb, Ni, Sn
New CSIR for New India
Development of Ductile Cu
based Bulk Metallic Glasses
DSC Curves of Cu-BMGs
Compressive stress strain curves
Compressive strength ~ 2100 to 2700 MPa & Plastic strain up to 16% obtained. A few alloys didn’t break and showed plastic strain >20%.

## Slide 9
Al coating by PVD process showed dense microstructures and good adhered interface.
Control of oxygen inside deposition chamber is crucial
Al coating by EC process using low cost ionic liquid showed good quality Al films.
Moisture control is crucial.
The process can be scaled up easily.
Electrochemical set up
Chrome passivated EC Al coat ings
Photograph of Al coated steel substrate
New CSIR for New India
Al Coatings for Cd Replacement

## Slide 10
Ti films on Si(100) substrate:(thickness: 140nm to 717nm)
Chakraborty et al. Acta mater. (2011) 59(7) 2615-2623
X-ray diffraction: Phase analysis
Texture evolution
Diffraction stress analysis
Conclusion
At low film thickness, high compressive stress (≥ 2 GPa) in hcp matrix may generate Shockley-partial dislocations which glide on close packed plane (00.2)hcp/(111)fcc in order to change the stacking sequence from hcp to fcc & vice versa.
Fcc phase is stable below a critical film thickness
Key observations
140nm
717nm
Rotationally symmetric biaxial stress
Fcc Ti: LP = 4.1638Å (this work)
LP = 4.11Å (ab initio calc.)PRB 65(2002)092106
Volume fraction of fcc Ti reduces with increasing film thickness.
Hence, hcp-fcc transformation is film thickness dependent
Texture evolution is driven by surface energy minimization
Compressive stress in hcp matrix decreases with increasing film thickness
New CSIR for New India
Hcp-fcc phase transformation
of Ti thin film

## Slide 11
Dip coating of Brass items
Advantages
Efficiency better than available lacquers
User friendly
  Can be used as dip coating, brush painting or spray coating
Cost effective
Outdoor Exposure test
New CSIR for New India
Anti-Tarnishing Lacquer for
Copper & its Alloys

## Slide 12
Blank
Saboo
CSIR-NML
24 Hours
Salt spray test (ASTM-B-117)
“Flower of Sulfur Test” (ASTM B 809)
20 days
Blank
CSIR-NML
Saboo
10 days
Blank
CSIR-NML
Saboo
0 hours
72 hours
Uncoated
Coated
New CSIR for New India
Accelerated Tarnish Test

## Slide 13
Inspiration from nature
WHY????
Ambient reaction conditions
Uniform morphology- site specific nucleation & growth
Reproducible Nanosize as matrix is defined
Monodispersity
Projects on two materials:
1. Nanosized hydroxyapatite & its various forms
2. Nanosized iron oxides and aqueous ferrofluids
New CSIR for New India
Biomaterials

## Slide 14
HA & β TCP
HA Powder
3-D HA Block
Microstructure
HA& β-TCP Powder
New CSIR for New India
Control Achieved over Morphology

## Slide 15
Characteristics of Hydroxyapatite | Sigma Aldrich, US | Kemix, US | Ningbo, China | NML
Form | Powder | Powder | Powder | Powder
Particle size | <200 nm | 40nm | 40nm | 25-30nm
Surface area | 10-15 m2/g | - | - | 67.54
bulk density g/cm3 | 2‑6 | - | - | 3.02
Trace elements (ppm) | - | - | - | <0.01
Cost | Rs 7000 | 56$ | 55$ | Rs 2000
Characteristics of Injectable Hydroxyapatite | BONESUPPORT™ | NML
Injectability/ working time | ≥ 4 min (through 16G cannulae) | 7-10 min
Final setting time | ≤ 45 min | 30 min
Compressive strength | 10 - 50 MPa | > 33 MPa
Setting reaction temp | < 43°C | < 30ºC
Hemocompatibility, Cytotoxicity, Initial screening &Sensitivity test, Cell adhesion-both in vitro & in vivo, Carcinogenesis evaluated and qualified
New CSIR for New India
Comparison with Commercial Brands

## Slide 16
Products Commercialized:
Nanosized Hydroxyapatite (Increased mechanical strength)
Nano HA+ β-tricalcium phosphate (Strength & Solubility)
Cover pages of journals
Industries with us
New CSIR for New India
Success Story

## Slide 17
FERROTEC’s EMG series, USA
Magnetite: 0.4-1.1% by vol
Size: 10nm
Dispersant:
not mentioned
0.5–1.5%by vol
Water: 97.4-99.1% by vol
Solubility in Water: Complete
Appearance & Odor: Black Fluid, no odor
Boiling Point (°F) 212° F
Specific Gravity 1.05 to1.07
Vapor Pressure (mm Hg.) 17 @20°C
Percent Volatile by Volume 97.4-99.1%
Vapor Density (AIR = 1) <1
Magnetisation: not mentioned
Colloidal Stability: not mentioned
Scale of production: not mentioned
NML’s BIOMATERIALS GROUP
Magnetite: 0.1- 0.3 % by vol (need to increase)
Size: ≤ 6nm
Dispersant:
biomolecules & water soluble polymers
0.05 – 2.5 % by volume
Water: 97-98% by vol
Solubility in water: Complete
Appearance &odour: Black, no odor
Specific Gravity (at rt)-0.996
Viscosity – 0.982
Boiling Point (°F) - 212° F
Magnetization: 0.23emu/gm
water soluble dried powder-43.34 emu/gm
Colloidal stability:
Zeta Pot:  -15 -18mV
Hydrodynamic diameter: 150-175nm
Polydispersity index: 0.1-0.2
Scale of production: one litre
Collaborative work with CCMB & BARC :feasibility studies for MRI & Hyperthermia
Hemocompatibility, Cytotoxicity, Initial screening &Sensitivity test, Cell adhesion-both in vitro & in vivo, Carcinogenesis evaluated and qualified
New CSIR for New India
Aqueous Ferrofluids