## Slide 1
Processing of Secondaries
& Waste

## Slide 2
Chart: 
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12
Sales | 12.5 | 12.5 | 12.5 | 12.5 | 12.5 | 12.5 | 12.5 | 12.5 | 12.5 | 12.5 | 12.5 | 12.5
Waste
Secondaries
Recovering metal values from secondaries
Converting waste into value added products
W from scrap
High purity Fe
from waste
Ni from
Spent Catalyst
Precious metals from E-waste
Rare earth extraction
And many
more…
Program on
fly ash utilization
Nonferrous slag
e.g. Cu, Zn, SiMn
Red mud utilization
Ferrous slag e.g.
steel slag, GBFS
Program on geopolymer
And many more…

## Slide 3
Recovering Metal Values from Secondaries

## Slide 4
Current Indian Scenario
High presence of Monazite in Indian beach sand (resource: 10.2 million tons)
Production of REs from monazite obtained from beach sand: 2700 tons/year
Current production by Indian Rare Earths Ltd. (IREL) : 7700 tons/year (2012 )
Composite chloride of REs (IREL) by hydrometallurgical route
IREL, Alwaye produces Misch metal & individual REs by SX/IX: Oxides of Y, La, Ce, Nd & Pr
India is the second largest supplier of yttrium in the world
Some separation process of other REs -heavy REs developed in India
Scope & Prospects of further R&D
Embargo on supply of REs from China – Provides opportunity for India
Indian Monazite is rich in REs (La, Ce, Pr, Nd, Sm) with small Gd (1%) & Y (0.1%)
Besides monazite, small Bastnaesite and Xenotime (rich in Y and heavy REs) deposits located in India & needs to be harnessed
Waste / secondary resources - spent catalysts, waste magnets, wind turbines are rich sources of REs and no proven extraction technology exists.
New CSIR for New India
Rare Earth Extraction

## Slide 5
Only about 1% of the total RE’s is reused and obsolete components are only recycled
Sl. No | Secondary material/ source | Metal values | Processing approach
1. | Super alloys of Ni and others | Nb, Ta, Re, Ni etc | Leaching- metal separation & recovery by SX
2. | Spent Li batteries | Rare earths, Li, Co & other metals | Leaching –metal separation & recovery by SX/IX
3. | Electronic wastes/ scraps- PCBs | Rare metals, Rare earths, PGMs | Hydrometallurgical processing
4. | Bayers’ liquor of alumina plants | Ga & other rare metals | Hydrometallurgy-SX/ IX
5 | Anode slime of copper electrolytic plants | Se, Te, PGMs, Ni etc | Pyrometallurgy / Leaching- Precipitation / SX/ IX
6. | Fly ash of gasification plants | Ga, Ge | Hydrometallurgy
7. | End-of life magnets from electronic equipments | Rare earths- Gd, Sm, Pd, Nd | Hydrometallurgy
8. | Monitors & Screens / LCDs | In | Hydrometallurgy- precipitation/ IX
9. | Sludge of alumina plant | V, Ga | Hydrometallurgy
10 | Spent petroleum catalysts | Mo, Co, V, PGMs | Hydrometallurgy- leaching- metal separation & recovery
New CSIR for New India
Secondaries for Recycling RE &
Rare Metals/ Energy Critical Elements

## Slide 6
New CSIR for New India
Activities under 12th Five Year Plan
Primary Resources (Indian Monazite)
Secondary Resources (Spent Catalyst)
Develop Novel Recovery process for Light REs (La, Ce, Pr, Nd, Sm) by SX using synergistic systems
Process package for leaching & separation of REs and other metals from waste catalysts
Process package for separation and recovery of individual light REs from Indian resources
Develop eco-friendly process (leaching-SX) to exploit spent catalyst for augmenting resource base of REs (La, Ce etc.) & base metals (Ni, Mo, Co)
Primary/Secondary RE resources

## Slide 7
Rare earth separation and recovery from Korean Monazite/ REO’s.
New CSIR for New India
Indo- Korean Cooperation
De-phosphotisation
Acid Leaching
Lanthanum
Praseodymium
Cerium
Neodymium
Solvent Extraction
Leach Liquor

## Slide 8
Ni : 9 - 21%, Al2O3: 40 - 85%
Nanosize
Ni-Zn ferrite
NiZnFe2O4, 30 nm
Nickel sulphate
Direct dissolution of Nickel from spent catalyst is difficult even with high strength acid and higher temperature
Ni : 20 - 75% Fe : 22 - 78%
Acid-3%, T -70 C
High pure alumina
New CSIR for New India
Nickel from Spent catalyst
A simple direct leaching method in presence of a promoter was developed with > 99% nickel recovery at low acid concentration

## Slide 9
Produce various shapes and sizes of hematite (200 – 4000 nm) from
Waste steel pickle liquor of Tata Steel
Titanium industry waste residue (Cochi)
Copper slag of Sterlite Industries
Crude iron oxide of Tata Steel
Manganese ferrous clay
Monodispersed & Uniform Size
Produce Mn-Zn ferrite from spent acid pickle liquor of steel industries
New CSIR for New India
High Purity Iron Oxide from Waste

## Slide 10
Dissolution
Ni-Cd Spent Battery
Cd, Co, Ni Separatn - SX
Mechanical separation
External case
Pure Metal
Electrolysis
Electrode material
Ni-Cd Ferrite
Hydroxide pptn
Iron removal
Alkali paste
Metal Oxide
Washing
Fe scrap
Paper/plastic
Dissolution
Hydroxide pptn
Hydrothermal conversion
Chart: Applied Field (G)
- Electrode material - 68.5%
- Case Material - 22.1%
- Paper - 3.8%
- Plastics - 0.63%
- Alkali – KOH - 3.25
Paper & Plastics
70% of world’s Cd is used in rechargeable batteries, Ni content is about 30%
Market share of mobile phones, Ni–Cd batteries 44.4%, lithium ion batteries 27.3%, NiMH batteries 28.0%
S L
Interesting Development :
Complete utilisation of battery components with >99% recovery
Better separation of Co-Ni using a combination of solvent mixture
Direct dissolution & pptn process to produce Ni-Cd ferrite
Ni | 41.7%
Cd | 24.3%
Co | 0.74%
Fe | 14.7%
Electrode material
Battery Fraction
New CSIR for New India
Spent Ni-Cd Battery Processing

## Slide 11
Lead Chloride
Pre-treatment
S L
Washing
Brine Leaching I
Brine leaching II
Cementation
Purification
S L
S L
Solid to Land Fill
Waste
Lead Cement
Balance water
Sulphuric Acid
For Zn & Cu recovery
Polishing
Iron Powder
)
)
Washing
Water
To be used as make-up water
)
Zn : 7.9%
Pb : 8.5%
Fe : 2.25%
Cu : 1.15%
Moist : 10.5%
Iron Powder
Zinc Plant Residue
Pb - 85 g, Zn - 79 g, Fe - 22.5 g, Cu-115 g
( Moist – 40%, Pb - 0.07%)
Crystallization
S L
S L
S L
Zinc secondary processing units generate huge quantity of residue containing lead
Lead is highly toxic and dumping is illegal
Environmental Authorities threaten to close the unit unless the residue is properly treated
Developed an environmental friendly process to recover lead
The process generates a final residue containing <0.1% Pb
New CSIR for New India
Pb Recovery from Zinc Plant Residue

## Slide 12
Precious metals 0.02%
Iron 20.47%
Lead 6.3%
Aluminum 14.17%
Copper 6.93%
Non-Metals 47.8%
Others 4.3%
Estimated generation in India - 10,00,000 MT in 2011
Will add up to 70, 000 MT of Cu and 200 MT of Precious Metals into the secondary stream.
Process developed on kilogram scale
Copper powder Silver powder
E-waste
Beneficiation
Pre-treatment
E-Waste Conc
Pressure Leaching
Lead Powder
Copper Powder
Precious metal recovery
Aeration Leaching
Oxidation Leaching
Gold Powder
Base metal recovery
Silver powder
New CSIR for New India
Metal Values from E-Waste

## Slide 13
Recycling of Li-ion batteries for recovery of cobalt and lithium
Dismantling and Separation
Cathode
Material
Waste Mobile
Batteries (LIBs)
Cobalt Salt
Leach Liquor
Solvent Extraction
15% Cyanex 272
Stripping H2SO4
Evaporation
Stripped
Solution
Lithium Salt
Evaporation
Raffinate
Leaching
Pulp density 100g/L, 2M H2SO4, Temp. 75 oC
Recovery of rare earth metal Nd from computer hard-disc
Leach Liquor
Precipitation
NaOH
Fe- Solution
Na-Nd double salt
20% HF
NdF3
(Value added Product)
Dismantled Hard-disc
Leaching of Magnet
Pulp density 100g/L,
2M H2SO4, Temp. 30 oC, Time 30 Min.
Magnet
New CSIR for New India
Metal Values from E-Waste

## Slide 14
A process for the removal of hazardous metal elements from leach liquor of electronic scraps following solvent extraction and recovery of valuables.
Sulfate Leach Solution
Cu, Zn, Cd, Ni
LIX84
H2SO4
HCl
Zn, Cd Extraction
pH=2.1
Zn, Cd, Ni Sol.
Ni Sol..n
Zn Sol..n
Cd Sol..n
Zn Stripping
Cd Stripping
Regenerated Cyanex 302
Cu Sol..n
Cu Extraction
pH= 1.91
Cu Stripping
H2SO4
New CSIR for New India
Indo- Korean Cooperation

## Slide 15
New CSIR for New India
Indo- Korean Cooperation
Recovery of Pb and Sn from the liberated resin of PCBs swelled by organic
PCBs
Metal Sheet (Cu)
Epoxy Resin (Pb, Sn)
Selective
Leaching
Lead Soln.
Tin Soln.
Metal free Epoxy resin for safe utilisation
n-methyl-2-pyrrolidone
Heat, S/L separation
HCl
HNO3
Organic Swelled PCBs
Highlights:
Novel pre-treatment organic swelling & liberation of pure Cu metal sheet
Energy saving process in comparison to traditional mechanical pre-treatment for metal beneficiation
Organic can be separated after swelling of PCBs and reused
Commercial viability after some scale-up studies

## Slide 16
Wealth from Waste

## Slide 17
Fly ash utilization in India
New CSIR for New India
Fly Ash Research
Opportunities for new technology
Summary of CSIR-NML’s activities

## Slide 18
Up to 120 MPa strength
Improved durability
Better abrasion resistance
High strength concrete from fly ash
Self glazed tiles from fly ash & GBFS
Conform EN Specs
Produced at 100◦C
Different colours & designs
As per IS 15658:2006
No leaching
Ready to use in 7 days
Paving blocks from fly ash, GBFS & red mud
New CSIR for New India
Geopolymer
Process Developed

## Slide 19
Fully automatic, with ~4 ton/shift capacity
Modular construction, both bricks and paving blocks can be produced
Supported by Department of Science & Technology
A step forward in translating process into technology
New CSIR for New India
Lab to Pilot Scale
Paving Blocks from Steel Slag
(jointly with Tata Steel)
50-55% steel slag can be used along with fly ash and granulated blast furnace slag,
Meet all the obligatory specification as per IS 15658: 2006,
Complied with the USEPA limit for leaching of toxic metals and is environmentally safe,
Breakthrough

## Slide 20
Technology transferred, plant operational from Nov 2011,
First commercialization of Geopolymer technology in India,
More than 500 tons of product has been produced,
Resulted into employment generation for 14 people,
Paving Blocks | Cement based | Steel slag based
Total CO2 generation / ton | 180 -200 kg (from firing of cement) | 16 - 20kg (conversion of alkali carbonate into oxide)
Water requirement/ ton | 300 liters | 250 liters
Waste & by-products reuse/ ton | <75 kg | >900 kg
Embodied energy/ kg | 1.2 MJ | 0.8 MJ
New CSIR for New India
Technology Commercialised

## Slide 21
Aluminium
Illmenite
Red Mud
Fly Ash
BF Slag
Zircon
Fundamental research
Leaching of MA ores
Novel reactors
Building materials
Large size mills
directions
Research Focus
New CSIR for New India
Mechanochemistry

## Slide 22
Lab Scale Development of Promising Processes
Fundamental Research
SMILE – A Simultaneous Milling and Leaching Process for Bauxites
Improved blended cements, PSC (80-85% BF slag) and PPC (50-55% fly ash)
High strength (~ 120 MPa) fly ash Geopolymers
Mechanical Activation of bauxite, Al-oxyhydroxides, illmenite, zircon, chromite, calcite, BF slag, fly ash
Energetics of milling, role of milling energy and water, interaction of minerals during milling
Texture induced surface charge modification during milling
Mechanical activation of porous minerals (e.g. boehmite)
Kinetics and mechanisms of reactions of activated minerals
Simulation of weathering processes
New CSIR for New India
Significant Achievements

## Slide 23
New CSIR for New India
Income 2008