## Slide 1: Current Activities at CSIR-NML on Steel

## Slide 2
Silt Erosion Resistant Steel for Turbine Hydrogenerator
High Strength High Formable Steels for Automobiles
Steels for Ultra Supercritical Boilers
API X80 Steel Development
Steel Research
Technology Development for CRGO Steels
Cementite Dissolution in Cold Drawn Pearlitic Steel
Low Temperature Sensitization & Intergranular Corrosion

## Slide 3
Francis Turbine
Damaged RUNNER due to Silt
Shark Bite
Developed material to have :
Corrosion resistance similar to 13%Cr4%Ni
Good Castability
Good Weldability
Improved Impact toughness property for resistance to cavitation erosion by silts
Improved abrasion and erosion resistance
for Turbine Hydrogenerator
New CSIR for New India
Silt Erosion Resistant Material

## Slide 4
New CSIR for New India
Process Flow Chart
Alloy Melting
(Vacuum Arc Melting of 40Kg)
Casting
Check homogeneity by chemical analysis and NDT (UT)
Characterization
Microstructural, Mechanical property
(Optical, SEM, TEM) (Tensile, Impact)
Heat Treatment at air atmosphere
Microstructural, mechanical property
Wear Study
(Solid particle Impingement, Cavitation)
Making of set up
Characterization after Wear
Scaling up to make prototype components
Structure-property correlation
Two Phase (Martensite + Austenite) Cr-Ni-Mn-Cu-Mo alloyed Steels developed for this application

## Slide 6
Variation of tensile strength with tempering temperature
13Cr-4Ni has tensile strength of 1000 MPa
13Cr-4Ni has impact toughness of 60-80J at room temperature
Variation of Impact toughness values with tempering temperature
Material is now undergoing field trial; components have been fabricated and will be put in the plant for the coming monsoon
New CSIR for New India
Properties

## Slide 7
  Design steel chemistry and processing parameters in order to get
    Yield Stress: 650 - 700 MPa
    Tensile Stress: 900-1000 MPa
    Uniform Elongation: 50% (Min.)
    Optimization of strength and formability
    Optimum balance between strength, fracture toughness and corrosion
Gaps Areas
Single phase TWIP was developed (UTS:700MPa; eu: 80%)
Two phase (ferrite + austenite)TWIP being developed takes care of Springback
Two phase TWIP cold rolled up to 90% at NML
Gap details
NML Work
No commercial production (POSCO
and ARCELOR have their own grades)
TWIP being high strength has high springback during processing
TWIP
New CSIR for New India
High Strength High Formable Steels

## Slide 8
New CSIR for New India
Process Flow Chart
Two Phase (Austenite + Ferrite) Mn-Cr-Al- alloyed Steels developed for this application
Alloy Melting
(Vacuum Arc Melting of 40Kg)
Hot forging followed by hot rolling (normal air cooling)
Characterization
Microstructural, Mechanical property
(Optical, SEM, TEM) (Tensile, Impact)
Cold rolling (11 passes) up to 90% reduction in thickness
Microstructural Characterization
Annealing at air atmosphere of 90% cold rolled sheet
Microstructural, Mechanical property
(Optical, SEM, TEM) (Tensile)
High strain rate testing for crash resistance & corrosion testing
Structure-property correlation

## Slide 9
Hot forged and hot rolled microstructure
{111}g
{110}a
{200}g
{200}a
{220}g
{311}g
{211}a
Only observed after 90% cold rolling
Necklace type structure: generally observed for dynamically recrystallized grains
Dynamic recrystallization is unlikely at room temperature
Chances of back transformation from ferrite to austenite is probable
New CSIR for New India
Process Flow Chart

## Slide 10
Sample Details | (YS) (MPa) | (UTS) (MPa) | (n-value) | Uniform Elongation
750 0C – 30 min. | 624 | 852 | 0.288 | 28
800 0C – 30 min. | 634 | 888 | 0.297 | 30
Unlike in the literature, shows no serration in the stress-strain plot at different strain rates
Chart: 
True Strain
True Stress, MPa
0
100
200
300
400
500
600
700
800
900
1000
0
0.05
0.1
0.15
0.2
0.25
0.3
0.35
0.4
Engineering strain
Engineering stress, MPa
strain rate = 2.5*10-4 s-1
750oC-30min
800oC-30min

## Slide 11
The FLD presented in the graph shows better forming properties compared to DP600
Forming limit diagram (FLD) has been determined from the annealed specimens along the rolling direction.

## Slide 12
Drawing strain:1.4
< 5 wt% cementite
Quantitative X-ray diffraction
Equilibrium weight fraction of cementite in pearlite: 12wt%
Quantitative XRD shows < 5wt% cementite at strain 1.4;
Conclusion: more than 50% cementite got dissolved
Drawing strain:0.12
Drawing strain:1.4
Drawing strain:1.4
Fragmented cementite
lamella and its
dissolution
Alternate ferrite and cementite lamella in pearlite
cementite lamella buckling
SEM micrograph
TEM micrograph
SEM micrograph
Drawn Pearlitic Steel
New CSIR for New India
Cementite Dissolution in Cold

## Slide 13
Role of ferrite dislocations in the dissolution
Traditional Williamson-Hall plot
Modified Williamson-Hall plot
(Ungar-Borbley )
Confirmation: Strain anisotropy due
to dislocations in the ferrite matrix
Non-monotonic increase of
FWHM with angle of diffraction
Strain 0.12: 44%screw + 56%edge
Strain: 1.4: 60%screw + 40%edge
Total avearge dislocation density: 6 x 1014/m2
Total avearge dislocation density: 8 x 1015/m2
Key results
Note: ferrite lattice parameter remains unchanged even after the dissolution. Hence, screw dislocations perhaps predominantly pull the carbon atoms from the cementite causing its dissolution.
CSIR-NML Tata Steel collaboration
Drawn Pearlitic Steel
New CSIR for New India
Cementite Dissolution in Cold

## Slide 14
Role of deformation, GBE, and welding on susceptibility to LTS, classical sensitization, IGC, and IGSCC
Prediction of LTS for 100 years at 300oC and Time-temperature-sensitization diagram
450C/1300h




MC
Deformation effects
Observations and outcome
Weld
Corrosion (IGC) of Stainless Steel
New CSIR for New India
Sensitization & Intergranular
Heat affected zone and base (304LN) are safe against IGC at 300oC for 100 years operation
Weld zones are susceptible to failure due to phase separation and LTS
Deformation e.g. >2.5% reduction in thickness causes IGC in 304LN

## Slide 15
Temperature, deg C
Time, h
BASE
Temperature, deg C
Time, h
HAZ
Temperature, deg C
Time, h
Weld
Note: TTS weld line separates fissured and non fissured regions
Note: TTS Base and HAZ line separates ‘step’ from ‘dual’ microstructure; assigned values are %DOS

## Slide 16
Designing of bulk nanostructure/ultrafine austenitic stainless steel
A novel Cyclic Strain Anneal process
for Bulk nano structure / ultra fine grain
Solution Annealed
Matrix
Cold
Deformation
Solution Annealed
Matrix
Cold
Deformation
Ultrafine Grained Stainless Steel
Recrystallisation
Recrystallisation
Isothermal
Thermal Cycle
gs< 200 nm
Present methods
Severe Plastic Deformation
Accumulative Roll Bonding
Repetitive Corrugation
Limitations ?
Increase in YS 3 to 4 times
Pub: Metall. Mater. Trans. A, 40, 2009, 3227
Mater Sci & Eng A 528, 2011, 2209

## Slide 17
Considère Criterion
Plastic instability
Poor strain hardenability &
Strain rate sensitivity
Ultra fine / nano structure Austenitic Stainless Steel -Deformation mechanism
UFG-I: Grain size
Below 500nm
Strain localization
UFG-II: Bimodal maxima at ~650nm and ~1400nm
Strain induced transformation of austenite to martensite
Bimodal grain size
Change in deformation mechanism
Concerns
Pub:Scripta Mater, 66,2012, 634

## Slide 18
Targeted properties
 Yield strength : 600-660 Mpa; YS/UTS ratio : 0.85-0.88;  Elongation : 20-25%
 Fracture Appearance Transition : -50 to -70 oC  Charpy Energy (-20 oC): 150-250 J
Challenges
► Coarse austenite grain size
► Limitation in temperature, strain and strain rate
► Criticality of composition selection (issues with Ti and Nb carbonitrides)
through Thin Slab Casting and Rolling (TSCR) – In collaboration with Tata Steel
For API grade steel
New CSIR for New India
API X80 Steel Development

## Slide 19
New CSIR for New India
Typical Process for API Grade Steel

## Slide 20
International Status : Very Few producers of HI-B CRGOs, no Indian producer
Indian Demand : ~ 1000 million USD worth
Justification/ Need :
It is not just developing another steel grade, but re-creation of a jealously guarded technology
Creation of a pilot scale integrated Flat Products development & processing facility – the only one of its kind in the country
Scale of operation: 3 – 5 Tonne per batch
CRGO Electrical Steel Sheets
New CSIR for New India
Technology Development for
Partnership : CSIR-Tata Steel-Ministry of Steel
(one of the largest PPP programmes ever)

## Slide 21
ICME: Processing-Structure-Property Correlation Models, Development of databases on composition-processing-microstructure-property correlation for steels
Design and development of high strength high formable steels for automotive applications
Design and development of pipeline steels.
Development of steels for application in USC boilers (30 MPa, 700oC Steam Conditions)
Fundamental understanding of deformation characteristics in steels
New CSIR for New India
Areas for Collaboration